Revisions made to the original MasterSpec text are made solely by the Licensee and are not endorsed by, or representative of the opinions of, Deltek or The American Institute of Architects (AIA). Neither AIA nor Deltek are liable in any way for such revisions or for the use of this Section by any end user. A qualified design professional should review and edit the document to suit project requirements.

SECTION 072500 - WEATHER BARRIERS

GENERAL

SUMMARY

Section Includes:

Mechanically-installed weather-resistive barrier.

GRIP-RITE® Commercial Grade-D Wrap.

Related accessories required for complete installation.

RELATED SECTIONS

Section 06 16 00 – Sheathing.

Section 07 21 00 – Thermal Insulation.

Section 07 62 00 – Sheet Metal Flashing and Trim.

Section 07 92 00 – Joint Sealants.

REFERENCES

A. ASTM E96 – Water Vapor Transmission of Materials.

B. AATCC 127 – Water Resistance: Hydrostatic Pressure Test.

C. ICC-ES AC38 – Acceptance Criteria for Weather-Resistive Barriers.

D. Applicable codes: IBC, IRC, IECC.

SUBMITTALS

A. Product data sheets and installation instructions.

B. Samples: Minimum 8-1/2 inch by 11 inch.

C. Warranty documentation, if applicable.

QUALITY ASSURANCE

A. Installer experienced with weather-resistive barrier systems.

B. Installation shall comply with manufacturer’s written instructions and applicable building codes.

DELIVERY, STORAGE, AND HANDLING

. Deliver materials in original packaging with labels intact.

B. Store in a dry, protected location, elevated off the ground.

C. Protect from prolonged UV exposure prior to installation.

PROJECT CONDITIONS

. Do not install over wet or frost-covered substrates.

B. Protect installed barrier from damage and weather until cladding is installed.

PRODUCTS

MANUFACTURER

Grip-Rite® / PrimeSource Building Products, Inc.

Website: www.grip-rite.com

MATERIALS

. GRIP-RITE® Commercial Grade-D Weather-Resistive Barrier

Description: Heavy-duty cross-woven polyethylene weather-resistive barrier designed for commercial and severe weather applications.

Composition: Cross-woven polyethylene with double-sided low-density polyethylene (LDPE) coating.

Performance Characteristics:

Resists bulk water intrusion.

Vapor permeable to promote wall drying.

Recognized air barrier material meeting IRC, IBC, and IECC requirements.

High tear, puncture, and break strength.

UV resistant up to 180 days.

Typical Physical Properties:

Basis weight: Approximately 120 g/m².

Water vapor permeance: Approximately 28 perms (ASTM E96).

Water penetration resistance: Approximately 400 cm H₂O (AATCC 127).

Color: White front; black back.

Roll Sizes: Standard commercial widths and lengths as provided by manufacturer.

ACCESSORIES

Fasteners: Corrosion-resistant nails, staples, or plastic cap fasteners.

Flashing: Compatible flashing membranes at openings and transitions.

Sealants and tapes compatible with polyethylene weather-resistive barriers.

EXECUTION

EXAMINATION

Verify substrates are sound, dry, and properly installed.

Correct unsatisfactory conditions prior to installation.

INSTALLATION OF WEATHER BARRIERS

Install in accordance with manufacturer’s instructions and applicable building codes.

Install horizontally, starting at base of wall and working upward in shingle fashion.

Provide minimum overlaps per manufacturer requirements.

Integrate with flashing at windows, doors, and penetrations to maintain continuous drainage plane.

Secure with approved fasteners at spacing recommended by manufacturer.

Repair damaged areas to maintain continuity.

PROTECTION

Cover with exterior cladding within 180 days of installation.

Replace material damaged beyond repair.

END OF SECTION 072500